Table S1. The composition of the prepared Semi-IPN hydrogels.

| Hydrogel | DEMAEMA (g) | Sodium alginate (g) | BisAA (g) | CaCl2 (% Wt./V) in water |
| --- | --- | --- | --- | --- |
| N1 | 1 | 1 | 0.2 | - |
| N2 | 2 | 1 | 0.4 | - |
| N3 | 3 | 1 | 0.6 | - |
| N4 | 1 | 1 | - | 0.5 |
| N5 | 1 | 2 | - | 0.5 |
| N6 | 1 | 3 | - | 0.5 |

Adsorption Isotherms

Ceqe=  1q max. Kl+ Ceq max               [4]

ln qe=lnKf+ 1nlnq.Ce                   [5]

Kinetics studies

lnqe-qt=lnq1-K1t                  [6]

tqt= 1K2.q2+ 1q2. t                         [7]

qt=Kp. t1l2 +C                              [8]

Adsorption Thermodynamics

lnK =∆S°R + ∆H°RT                       [9]

∆G°=∆H-T∆S°                        [10]

Figure S1. The swelling ratios of N1-N3 as a function of time

Figure S2. The swelling ratios of N4-N6 at equilibrium state.

Figure S3. BET and BJH of N3 and N4.

Figure S4. DSC and TGA thermograms of N3 and N4.

Table S2. Thermal analysis data of N3 and N4.

| Hydrogel | 1st decomposition state |  |  | 2nd decomposition state |  |  | T50% oC | Char content at 600 oC (%) | Tg oC |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ti | Tf | Rate of Decomp. % wt / min | Ti | Tf | Rate of Decomp. % wt / min |  |  |  |
| N3 | 208 | 312 | 0.350 | 372 | 442 | 0.355 | 360 | 21.62 | 93.13 |
| N4 | 211 | 309 | 0.318 | 319 | 447 | 0.080 | 324 | 32.95 | 87.17 |

Figure S5. The Langmuir isotherm of CR dye adsorption on the CR dye on prepared N3 and N4 at 35°C.

Figure S6. The Freundlich isotherm of CR dye adsorption on the CR dye on prepared N3 and N4 at 35°C.

Figure S7. The pseudo-first-order kinetic for the adsorption of CR dye on N3 and N4.

Table S3. The parameters of Pseudo-first order for the adsorption of CR dye on N3 and N4.

| K1/N4 | q(theo) | q(exp) | R2/N4 | K1/N3 | q(theo) | q(exp) | R2/N3 | T (0C) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0282 | 583.883 | 1171 | 0.8815 | 0.0227 | 84.1499 | 1216 | 0.9116 | 35 |
| 0.0216 | 448.496 | 1260 | 0.9668 | 0.0637 | 133.166 | 1303 | 0.8218 | 45 |
| 0.0237 | 144.676 | 1328 | 0.9055 | 0.1225 | 201.1 | 1365 | 0.7337 | 65 |

Figure S8. Pseudo-second-order kinetic for the adsorption of CR dye on N3 and N4.

Table S4. The parameters of Pseudo-second-order for the adsorption of CR dye on N3 and N4.

| q(theo) | q(exp) | K2/N3 | R2/N3 | q(theo) | q (exp) | K2/N3 | R2/N3 | T(0C) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1250 | 1170.7 | 3.84E-09 | 0.8815 | 1250 | 1216 | 2.75E-09 | 0.9976 | 35 |
| 1250 | 1259.7 | 2.94E-09 | 0.9668 | 1250 | 1303 | 1.86E-09 | 0.9985 | 45 |
| 1428.57 | 1328 | 4.41E-10 | 0.9055 | 1428.571 | 1365 | 5.39E-10 | 0.9998 | 65 |

Figure S9. Intra-particle diffusion kinetic for adsorption of CR dye on N3 and N4.

Table S5. The parameters of intra-particle diffusion for CR adsorption on N3 and N4.

| Kp/N4 | I/N4 | R2/N4 | Kp/N3 | I/N3 | R2/N3 | T (0C) |
| --- | --- | --- | --- | --- | --- | --- |
| 46.325 | 643.59 | 0.928 | 26.543 | 1743.6 | 0.8599 | 35 |
| 39.816 | 795.82 | 0.9598 | 27.673 | 1662.8 | 0.9284 | 45 |
| 17.864 | 1146.9 | 0.8694 | 21.52 | 1542.1 | 0.7952 | 65 |

Figure S10. Thermodynamic for adsorption of CR on N3 and N4.

Table S6. The thermodynamic factors and variables for CR dye adsorption on the N3 and N4.

| ΔG˚ (kJ/mol.K) | ΔE˚ (kJ/mol.K) | ΔS˚ (J/mol.K) | ΔH˚ (kJ/mol. K) | Temp. (oK) | Hydrogel |
| --- | --- | --- | --- | --- | --- |
| -4.924 | 48.083 | 181.95 | 51.144 | 308.15 | N3 |
| -6.744 |  |  |  | 318.15 |  |
| -10.38 |  |  |  | 338.15 |  |
| -4.29 | 40.549 | 132.400 | 36.506 | 308.15 | N4 |
| -5.61 |  |  |  | 318.15 |  |
| -8.26 |  |  |  | 338.15 |  |

Figure S11. detect activation energy for adsorption of CR dye on N3 and N4.